RTCD296  SERIES　　　（ 105℃ 5000H）

- Compliant to the RoHS directive.

- 105℃ 5000H long life and high ripple current series.

- Used in professional power supplies and frequency converters etc.

■Specification

| Item | Performance Characteristics |
| --- | --- |
| Operating range | -40℃～+105℃ | -25℃～+105℃ |
| Rated voltage range | 16V～100V | 160V～450V |
| Capacitance tolerance | ±20% (20℃, 120Hz) |
| Leakage current | I≤0.01CV(μA) or1.5mA (Whichever is smaller) (20℃, after 5 minutes) C=Nominal capacitance(μF), V=Rated voltage(V) |
| Dissipation factor (20℃，120Hz) | UR(V) 16 25 35 50 63 80 100 160～250 350～400 450 tanδ 0.50 0.45 0.40 0.35 0.30 0.25 0.20 0.15 0.20 0.25 |
| Stability at Low Temperature (Impedance ratio at120Hz) | UR(V) 16～100 160～250 315～450 Z(-25℃)/Z(+20℃) 4 3 8 Z(-40℃)/Z(+20℃) 15 - |
| Load Life | After applying rated voltage with specified ripple current for 2000 hours at 85℃(the peak voltage shall not exceed the rated voltage), and then restored for 24 hours, capacitor shall meet the following requirement: Capacitance change Within ±20% of the initial value. Dissipation factor Not more than 200% of the initial specified value. Leakage current Not more than the initial specified value. |
| Shelf Life | After storing for 1000 hours at 85℃,UR to be applied for 30 minutes and then restored for 24 hours, capacitor shall meet the following requirement: Capacitance change Within ±20% of the initial value. Dissipation factor Not more than 200% of the initial specified value. Leakage current Not more than the initial specified value. |
| Standard | JIS C 5101-4 |

■Coefficient of rated ripple current

| 温度(℃) | 40 | 55 | 70 | 85 | 105 |  | 频率(Hz) UR(V) | 50(60) | 120 | 500 | 1K | ≥10K |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 系数 | 2.7 | 2.5 | 2.1 | 1.7 | 1.0 |  | 16-100 | 0.90 | 1.00 | 1.05 | 1.10 | 1.15 |
|  |  |  |  |  |  |  | 160-250 | 0.80 | 1.00 | 1.20 | 1.30 | 1.50 |
|  |  |  |  |  |  |  | 315-450 | 0.80 | 1.00 | 1.20 | 1.25 | 1.40 |

■Drawing                                Unit：mm

*:Shorter terminal is: 4.0±0.5mm

■RTCD296 Dimensions

| Rated Voltage code (V.DC) | Capacitance ( μF) | Case size ΦD×L(mm) | tanδ 20℃, 120Hz | Ripple current 105℃, 120Hz (Arms) | Max ESR 20℃, 120Hz (mΩ) | ESR(typ.) 20℃, 120Hz (mΩ) | Part number |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 16 1C (20) | 5600 | 22*30 | 0.50 | 1.49 | 120 | 85 | RTCD2961C562KP030M |
|  | 6800 | 22*30 | 0.50 | 1.66 | 100 | 70 | RTCD2961C682KP030M |
|  | 8200 | 25*30 | 0.50 | 1.71 | 90 | 60 | RTCD2961C822KQ030M |
|  | 10000 | 22*35 | 0.50 | 2.10 | 70 | 50 | RTCD2961C103KP035M |
|  |  | 25*30 | 0.50 | 2.08 | 70 | 50 | RTCD2961C103KQ030M |
|  | 12000 | 22*40 | 0.50 | 23.60 | 60 | 40 | RTCD2961C123KP040M |
|  |  | 25*35 | 0.50 | 2.38 | 60 | 40 | RTCD2961C123KQ035M |
|  |  | 30*30 | 0.50 | 2.35 | 60 | 40 | RTCD2961C123KR030M |
|  | 15000 | 22*45 | 0.50 | 2.67 | 45 | 35 | RTCD2961C153KP045M |
|  |  | 25*40 | 0.50 | 2.72 | 45 | 35 | RTCD2961C153KQ040M |
|  | 18000 | 25*45 | 0.50 | 3.06 | 40 | 30 | RTCD2961C183KQ045M |
|  |  | 30*35 | 0.50 | 3.03 | 40 | 30 | RTCD2961C183KR035M |
|  |  | 35*30 | 0.50 | 3.10 | 40 | 30 | RTCD2961C183KS030M |
|  | 22000 | 25*50 | 0.50 | 3.40 | 30 | 22 | RTCD2961C223KQ050M |
|  |  | 30*40 | 0.50 | 3.46 | 30 | 22 | RTCD2961C223KR040M |
|  | 27000 | 30*45 | 0.50 | 3.89 | 25 | 18 | RTCD2961C273KR045M |
|  |  | 35*35 | 0.50 | 3.86 | 25 | 18 | RTCD2961C273KS035M |
|  | 33000 | 30*50 | 0.50 | 4.33 | 20 | 15 | RTCD2961C333KR050M |
|  |  | 35*40 | 0.50 | 4.33 | 20 | 15 | RTCD2961C333KS040M |
|  | 39000 | 35*45 | 0.50 | 4.96 | 18 | 13 | RTCD2961C393KS045M |
|  | 47000 | 35*50 | 0.50 | 5.49 | 15 | 11 | RTCD2961C473KS050M |
|  | 56000 | 35*50 | 0.50 | 5.38 | 15 | 9 | RTCD2961C563KS050M |
| 25 1E (32) | 3900 | 22*25 | 0.45 | 1.32 | 160 | 110 | RTCD2961E392KP025M |
|  | 4700 | 22*30 | 0.45 | 1.56 | 130 | 90 | RTCD2961E472KP030M |
|  | 5600 | 22*35 | 0.45 | 1.78 | 110 | 75 | RTCD2961E562KP035M |
|  |  | 25*25 | 0.45 | 1.77 | 110 | 75 | RTCD2961E562KQ025M |
|  | 6800 | 22*40 | 0.45 | 2.02 | 90 | 65 | RTCD2961E682KP040M |
|  |  | 25*30 | 0.45 | 1.89 | 90 | 65 | RTCD2961E682KQ030M |
|  | 8200 | 22*45 | 0.45 | 2.28 | 75 | 55 | RTCD2961E822KP045M |
|  |  | 25*35 | 0.45 | 2.18 | 75 | 55 | RTCD2961E822KQ035M |
|  |  | 30*30 | 0.45 | 2.23 | 75 | 55 | RTCD2961E822KR030M |
|  | 10000 | 22*50 | 0.45 | 2.56 | 60 | 45 | RTCD2961E103KP050M |
|  |  | 25*40 | 0.45 | 2.54 | 60 | 45 | RTCD2961E103KQ040M |
|  | 12000 | 25*45 | 0.45 | 2.79 | 50 | 35 | RTCD2961E123KQ045M |
|  |  | 30*35 | 0.45 | 2.72 | 50 | 35 | RTCD2961E123KR035M |
|  |  | 35*30 | 0.45 | 2.76 | 50 | 35 | RTCD2961E123KS030M |
|  | 15000 | 30*40 | 0.45 | 3.13 | 40 | 30 | RTCD2961E153KR040M |
|  | 18000 | 30*45 | 0.45 | 3.52 | 35 | 25 | RTCD2961E183KR045M |
|  | 22000 | 30*50 | 0.45 | 3.93 | 30 | 20 | RTCD2961E223KR050M |
|  |  | 35*40 | 0.45 | 3.95 | 30 | 20 | RTCD2961E223KS040M |
|  | 27000 | 35*50 | 0.45 | 4.73 | 25 | 18 | RTCD2961E273KS050M |
| 35 1V (44) | 2700 | 22*25 | 0.40 | 1.30 | 200 | 140 | RTCD2961V272KP025M |
|  | 3300 | 22*30 | 0.40 | 1.55 | 170 | 120 | RTCD2961V332KP030M |
|  | 3900 | 22*35 | 0.40 | 1.77 | 140 | 95 | RTCD2961V392KP035M |
|  |  | 25*25 | 0.40 | 1.76 | 140 | 95 | RTCD2961V392KQ025M |
|  | 4700 | 22*40 | 0.40 | 2.02 | 120 | 80 | RTCD2961V472KP040M |
|  |  | 25*30 | 0.40 | 1.98 | 120 | 80 | RTCD2961V472KQ030M |
|  | 5600 | 22*45 | 0.40 | 2.26 | 100 | 70 | RTCD2961V562KP045M |
|  |  | 25*35 | 0.40 | 2.18 | 100 | 70 | RTCD2961V562KQ035M |
|  |  | 30*30 | 0.40 | 2.12 | 100 | 70 | RTCD2961V562KR030M |
|  | 6800 | 22*50 | 0.40 | 2.50 | 80 | 55 | RTCD2961V682KP050M |
|  |  | 25*40 | 0.40 | 2.46 | 80 | 55 | RTCD2961V682KQ040M |
|  | 8200 | 25*45 | 0.40 | 2.81 | 65 | 45 | RTCD2961V822KQ045M |
|  |  | 30*35 | 0.40 | 2.70 | 65 | 45 | RTCD2961V822KR035M |
|  | 10000 | 30*40 | 0.40 | 3.04 | 55 | 40 | RTCD2961V103KR040M |
|  |  | 35*30 | 0.40 | 2.80 | 55 | 40 | RTCD2961V103KS030M |
|  | 12000 | 30*45 | 0.40 | 3.39 | 45 | 35 | RTCD2961V123KR045M |
|  |  | 35*35 | 0.40 | 3.30 | 45 | 35 | RTCD2961V123KS035M |
|  | 15000 | 35*40 | 0.40 | 3.38 | 35 | 25 | RTCD2961V153KS040M |
|  | 18000 | 35*45 | 0.40 | 4.40 | 30 | 21 | RTCD2961V183KS045M |

| Rated Voltage code (V.DC) | Capacitance ( μF) | Case size ΦD×L(mm) | tanδ 20℃, 120Hz | Ripple current 105℃, 120Hz (Arms) | Max ESR 20℃, 120Hz (mΩ) | ESR(typ.) 20℃, 120Hz (mΩ) | Part number |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 50 1H (63) | 1500 | 22*25 | 0.35 | 1.21 | 310 | 220 | RTCD2961H152KP025M |
|  | 2200 | 22*30 | 0.35 | 1.53 | 215 | 150 | RTCD2961H222KP030M |
|  | 2700 | 25*30 | 0.35 | 1.77 | 175 | 120 | RTCD2961H272KQ030M |
|  | 3300 | 22*40 | 0.35 | 1.92 | 145 | 100 | RTCD2961H332KP040M |
|  |  | 30*25 | 0.35 | 1.92 | 145 | 100 | RTCD2961H332KR025M |
|  | 3900 | 25*40 | 0.35 | 2.23 | 120 | 85 | RTCD2961H392KQ040M |
|  |  | 30*30 | 0.35 | 2.20 | 120 | 85 | RTCD2961H392KR030M |
|  | 4700 | 25*45 | 0.35 | 2.46 | 100 | 70 | RTCD2961H472KQ045M |
|  | 5600 | 30*40 | 0.35 | 2.72 | 85 | 60 | RTCD2961H562KR040M |
|  |  | 35*30 | 0.35 | 2.59 | 85 | 60 | RTCD2961H562KS030M |
|  | 6800 | 30*45 | 0.35 | 3.02 | 70 | 50 | RTCD2961H682KR045M |
|  |  | 35*35 | 0.35 | 2.92 | 70 | 50 | RTCD2961H682KS035M |
|  | 8200 | 30*50 | 0.35 | 3.63 | 60 | 40 | RTCD2961H822KR050M |
|  |  | 35*40 | 0.35 | 3.37 | 60 | 40 | RTCD2961H822KS040M |
|  | 10000 | 35*45 | 0.35 | 3.80 | 50 | 35 | RTCD2961H103KS045M |
|  | 12000 | 35*50 | 0.35 | 4.07 | 40 | 30 | RTCD2961H123KS050M |
| 63 1J (79) | 1500 | 25*30 | 0.30 | 1.42 | 270 | 190 | RTCD2961J152KQ030M |
|  | 1800 | 22*35 | 0.30 | 1.63 | 230 | 160 | RTCD2961J182KP035M |
|  | 2200 | 22*40 | 0.30 | 1.86 | 185 | 130 | RTCD2961J222KP040M |
|  |  | 30*25 | 0.30 | 1.81 | 185 | 130 | RTCD2961J222KR025M |
|  | 2700 | 25*40 | 0.30 | 2.04 | 150 | 110 | RTCD2961J272KQ040M |
|  |  | 30*30 | 0.30 | 2.02 | 150 | 110 | RTCD2961J272KR030M |
|  | 3300 | 25*45 | 0.30 | 2.39 | 125 | 85 | RTCD2961J332KQ045M |
|  | 3900 | 30*35 | 0.30 | 2.47 | 110 | 75 | RTCD2961J392KR035M |
|  |  | 35*30 | 0.30 | 2.32 | 110 | 75 | RTCD2961J392KS030M |
|  | 4700 | 30*45 | 0.30 | 2.85 | 90 | 60 | RTCD2961J472KR045M |
|  |  | 35*35 | 0.30 | 2.78 | 90 | 60 | RTCD2961J472KS035M |
|  | 5600 | 30*50 | 0.30 | 3.28 | 75 | 50 | RTCD2961J562KR050M |
|  |  | 35*40 | 0.30 | 3.20 | 75 | 50 | RTCD2961J562KS040M |
|  | 6800 | 35*45 | 0.30 | 3.62 | 60 | 60 | RTCD2961J682KS045M |
|  | 8200 | 35*50 | 0.30 | 3.95 | 50 | 35 | RTCD2961J822KS050M |
| 80 1K (100) | 820 | 22*25 | 0.25 | 1.10 | 410 | 290 | RTCD2961K821KP025M |
|  | 1000 | 22*30 | 0.25 | 1.29 | 335 | 235 | RTCD2961K102KP030M |
|  | 1200 | 22*35 | 0.25 | 1.49 | 280 | 195 | RTCD2961K122KP035M |
|  |  | 25*25 | 0.25 | 1.39 | 280 | 195 | RTCD2961K122KQ025M |
|  | 1500 | 25*30 | 0.25 | 1.75 | 225 | 160 | RTCD2961K152KQ030M |
|  |  | 30*30 | 0.25 | 1.78 | 225 | 160 | RTCD2961K152KR030M |
|  | 1800 | 22*45 | 0.25 | 1.92 | 185 | 130 | RTCD2961K182KP045M |
|  |  | 25*35 | 0.25 | 1.86 | 185 | 130 | RTCD2961K182KQ035M |
|  | 2200 | 25*45 | 0.25 | 2.22 | 155 | 110 | RTCD2961K222KQ045M |
|  |  | 30*35 | 0.25 | 2.08 | 155 | 110 | RTCD2961K222KR035M |
|  | 2700 | 30*40 | 0.25 | 2.40 | 130 | 90 | RTCD2961K272KR040M |
|  |  | 35*30 | 0.25 | 2.46 | 130 | 90 | RTCD2961K272KS030M |
|  | 3300 | 30*40 | 0.25 | 2.70 | 110 | 70 | RTCD2961K332KR040M |
|  |  | 35*35 | 0.25 | 2.61 | 110 | 70 | RTCD2961K332KS035M |
|  | 3900 | 30*45 | 0.25 | 2.95 | 85 | 60 | RTCD2961K392KR045M |
|  |  | 35*40 | 0.25 | 3.01 | 85 | 60 | RTCD2961K392KS040M |
|  | 4700 | 35*45 | 0.25 | 3.45 | 75 | 50 | RTCD2961K472KS045M |
|  | 5600 | 35*50 | 0.25 | 3.73 | 60 | 45 | RTCD2961K562KS050M |
| 100 2A (125) | 560 | 22*25 | 0.20 | 1.01 | 480 | 335 | RTCD2962A561KP025M |
|  | 820 | 22*35 | 0.20 | 1.34 | 330 | 230 | RTCD2962A821KP035M |
|  |  | 25*25 | 0.20 | 1.28 | 330 | 230 | RTCD2962A821KQ025M |
|  | 1000 | 22*40 | 0.20 | 1.58 | 265 | 190 | RTCD2962A102KP040M |
|  |  | 25*35 | 0.20 | 1.56 | 265 | 190 | RTCD2962A102KQ035M |
|  | 1200 | 22*45 | 0.20 | 1.76 | 225 | 160 | RTCD2962A122KP045M |
|  |  | 25*40 | 0.20 | 1.79 | 225 | 160 | RTCD2962A122KQ040M |
|  | 1500 | 22*50 | 0.20 | 2.00 | 180 | 130 | RTCD2962A152KP050M |
|  |  | 25*45 | 0.20 | 2.06 | 180 | 130 | RTCD2962A152KQ045M |
|  | 1800 | 30*35 | 0.20 | 2.20 | 150 | 110 | RTCD2962A182KR035M |
|  |  | 35*30 | 0.20 | 2.16 | 150 | 110 | RTCD2962A182KS030M |
|  | 2200 | 30*40 | 0.20 | 2.52 | 125 | 90 | RTCD2962A222KR040M |
|  |  | 35*35 | 0.20 | 2.49 | 125 | 90 | RTCD2962A222KS035M |
|  | 2700 | 30*45 | 0.20 | 2.86 | 100 | 70 | RTCD2962A272KR045M |
|  |  | 35*40 | 0.20 | 2.88 | 100 | 70 | RTCD2962A272KS040M |
|  | 3300 | 35*45 | 0.20 | 3.25 | 80 | 60 | RTCD2962A332KS045M |
|  | 3900 | 35*50 | 0.20 | 3.57 | 70 | 50 | RTCD2962A392KS050M |

| Rated Voltage code (V.DC) | Capacitance ( μF) | Case size ΦD×L(mm) | tanδ 20℃, 120Hz | Ripple current 105℃, 120Hz (Arms) | Max ESR 20℃, 120Hz (mΩ) | ESR(typ.) 20℃, 120Hz (mΩ) | Part number |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 160 2C (200) | 220 | 22*25 | 0.15 | 0.63 | 910 | 635 | RTCD2962C221KP025M |
|  | 270 | 22*30 | 0.15 | 0.76 | 740 | 520 | RTCD2962C271KP030M |
|  | 330 | 22*35 | 0.15 | 0.95 | 610 | 425 | RTCD2962C331KP035M |
|  |  | 25*25 | 0.15 | 0.85 | 610 | 425 | RTCD2962C331KQ025M |
|  | 390 | 25*30 | 0.15 | 0.97 | 510 | 360 | RTCD2962C391KQ030M |
|  |  | 30*25 | 0.15 | 1.05 | 510 | 360 | RTCD2962C391KR025M |
|  | 470 | 22*40 | 0.15 | 1.11 | 425 | 300 | RTCD2962C471KP040M |
|  |  | 25*35 | 0.15 | 1.15 | 425 | 300 | RTCD2962C471KQ035M |
|  |  | 30*30 | 0.15 | 1.18 | 425 | 300 | RTCD2962C471KR030M |
|  | 560 | 22*45 | 0.15 | 1.27 | 355 | 250 | RTCD2962C561KP045M |
|  | 680 | 22*50 | 0.15 | 1.44 | 300 | 210 | RTCD2962C681KP050M |
|  |  | 25*40 | 0.15 | 1.44 | 300 | 210 | RTCD2962C681KQ040M |
|  |  | 30*35 | 0.15 | 1.51 | 300 | 210 | RTCD2962C681KR035M |
|  | 820 | 25*45 | 0.15 | 1.63 | 245 | 170 | RTCD2962C821KQ045M |
|  |  | 30*40 | 0.15 | 1.67 | 245 | 170 | RTCD2962C821KR040M |
|  |  | 35*30 | 0.15 | 1.63 | 245 | 170 | RTCD2962C821KS030M |
|  | 1000 | 30*45 | 0.15 | 1.90 | 200 | 140 | RTCD2962C102KR045M |
|  |  | 35*35 | 0.15 | 1.90 | 200 | 140 | RTCD2962C102KS035M |
|  | 1200 | 30*50 | 0.15 | 2.16 | 170 | 120 | RTCD2962C122KR050M |
|  |  | 35*40 | 0.15 | 2.23 | 170 | 120 | RTCD2962C122KS040M |
|  | 1500 | 35*45 | 0.15 | 2.61 | 135 | 100 | RTCD2962C152KS045M |
|  | 1800 | 35*50 | 0.15 | 2.98 | 115 | 80 | RTCD2962C182KS050M |
| 180 2K (225) | 220 | 22*25 | 0.15 | 0.63 | 910 | 635 | RTCD2962K221KP025M |
|  | 270 | 22*30 | 0.15 | 0.76 | 740 | 520 | RTCD2962K271KP030M |
|  | 330 | 22*35 | 0.15 | 0.91 | 610 | 520 | RTCD2962K331KP035M |
|  |  | 25*30 | 0.15 | 0.91 | 610 | 425 | RTCD2962K331KQ030M |
|  | 390 | 22*40 | 0.15 | 1.03 | 510 | 425 | RTCD2962K391KP040M |
|  |  | 25*35 | 0.15 | 1.06 | 510 | 360 | RTCD2962K391KQ035M |
|  |  | 30*25 | 0.15 | 1.03 | 510 | 360 | RTCD2962K391KR025M |
|  | 470 | 22*45 | 0.15 | 1.18 | 425 | 360 | RTCD2962K471KP045M |
|  |  | 30*30 | 0.15 | 1.18 | 425 | 300 | RTCD2962K471KR030M |
|  | 560 | 22*50 | 0.15 | 1.33 | 355 | 300 | RTCD2962K561KP050M |
|  |  | 25*40 | 0.15 | 1.33 | 355 | 250 | RTCD2962K561KQ040M |
|  |  | 30*35 | 0.15 | 1.33 | 355 | 250 | RTCD2962K561KR035M |
|  | 680 | 25*45 | 0.15 | 1.52 | 300 | 205 | RTCD2962K681KQ045M |
|  |  | 35*30 | 0.15 | 1.49 | 300 | 205 | RTCD2962K681KS030M |
|  | 820 | 25*50 | 0.15 | 1.72 | 245 | 170 | RTCD2962K821KQ050M |
|  |  | 30*40 | 0.15 | 1.75 | 245 | 170 | RTCD2962K821KR040M |
|  |  | 35*35 | 0.15 | 1.76 | 245 | 170 | RTCD2962K821KS035M |
|  | 1000 | 30*45 | 0.15 | 2.02 | 200 | 140 | RTCD2962K102KR045M |
|  |  | 35*40 | 0.15 | 2.08 | 200 | 140 | RTCD2962K102KS040M |
|  | 1200 | 30*50 | 0.15 | 2.25 | 170 | 120 | RTCD2962K122KR050M |
|  |  | 35*45 | 0.15 | 2.24 | 170 | 120 | RTCD2962K122KS045M |
|  | 1500 | 35*50 | 0.15 | 2.77 | 135 | 95 | RTCD2962K152KS050M |
| 200 2D (250) | 180 | 22*25 | 0.15 | 0.57 | 1110 | 780 | RTCD2962D181KP025M |
|  | 220 | 22*30 | 0.15 | 0.72 | 910 | 640 | RTCD2962D221KP030M |
|  | 270 | 22*35 | 0.15 | 0.84 | 740 | 520 | RTCD2962D271KP035M |
|  |  | 25*25 | 0.15 | 0.77 | 740 | 520 | RTCD2962D271KQ025M |
|  | 330 | 22*40 | 0.15 | 0.97 | 610 | 430 | RTCD2962D331KP040M |
|  |  | 25*30 | 0.15 | 0.91 | 610 | 430 | RTCD2962D331KQ030M |
|  | 390 | 25*35 | 0.15 | 1.07 | 510 | 360 | RTCD2962D391KQ035M |
|  |  | 30*25 | 0.15 | 1.03 | 510 | 360 | RTCD2962D391KR025M |
|  | 470 | 25*40 | 0.15 | 1.23 | 425 | 300 | RTCD2962D471KQ040M |
|  |  | 30*30 | 0.15 | 1.18 | 425 | 300 | RTCD2962D471KR030M |
|  | 560 | 25*45 | 0.15 | 1.40 | 355 | 250 | RTCD2962D561KQ045M |
|  |  | 30*35 | 0.15 | 1.39 | 355 | 250 | RTCD2962D561KR035M |
|  | 680 | 25*50 | 0.15 | 1.59 | 295 | 210 | RTCD2962D681KQ050M |
|  |  | 30*40 | 0.15 | 1.61 | 295 | 210 | RTCD2962D681KR040M |
|  |  | 35*30 | 0.15 | 1.50 | 295 | 210 | RTCD2962D681KS030M |
|  | 820 | 30*45 | 0.15 | 1.86 | 245 | 170 | RTCD2962D821KR045M |
|  |  | 35*35 | 0.15 | 1.76 | 245 | 170 | RTCD2962D821KS035M |
|  | 1000 | 30*50 | 0.15 | 2.12 | 200 | 140 | RTCD2962D102KR050M |
|  |  | 35*40 | 0.15 | 2.08 | 200 | 140 | RTCD2962D102KS040M |
|  | 1200 | 35*45 | 0.15 | 2.38 | 170 | 120 | RTCD2962D122KS045M |
|  | 1500 | 35*50 | 0.15 | 2.77 | 140 | 100 | RTCD2962D152KS050M |

| Rated Voltage code (V.DC) | Capacitance ( μF) | Case size ΦD×L(mm) | tanδ 20℃, 120Hz | Ripple current 105℃, 120Hz (Arms) | Max ESR 20℃, 120Hz (mΩ) | ESR(typ.) 20℃, 120Hz (mΩ) | Part number |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 250 2E (300) | 150 | 22*25 | 0.15 | 0.52 | 1330 | 930 | RTCD2962E151KP025M |
|  | 180 | 22*30 | 0.15 | 0.64 | 1110 | 780 | RTCD2962E181KP030M |
|  | 220 | 22*35 | 0.15 | 0.76 | 910 | 640 | RTCD2962E221KP035M |
|  |  | 25*30 | 0.15 | 0.76 | 910 | 640 | RTCD2962E221KQ030M |
|  | 270 | 22*40 | 0.15 | 0.88 | 740 | 520 | RTCD2962E271KP040M |
|  |  | 25*35 | 0.15 | 0.90 | 740 | 520 | RTCD2962E271KQ035M |
|  |  | 30*25 | 0.15 | 0.85 | 740 | 520 | RTCD2962E271KR025M |
|  | 330 | 22*45 | 0.15 | 1.01 | 610 | 425 | RTCD2962E331KP045M |
|  |  | 30*30 | 0.15 | 1.00 | 610 | 425 | RTCD2962E331KR030M |
|  | 390 | 22*50 | 0.15 | 1.14 | 510 | 360 | RTCD2962E391KP050M |
|  |  | 25*40 | 0.15 | 1.14 | 510 | 360 | RTCD2962E391KQ040M |
|  |  | 30*35 | 0.15 | 1.16 | 510 | 360 | RTCD2962E391KR035M |
|  | 470 | 25*45 | 0.15 | 1.30 | 425 | 300 | RTCD2962E471KQ045M |
|  |  | 35*30 | 0.15 | 1.25 | 425 | 300 | RTCD2962E471KS030M |
|  | 560 | 25*50 | 0.15 | 1.46 | 355 | 250 | RTCD2962E561KQ050M |
|  |  | 30*40 | 0.15 | 1.49 | 355 | 250 | RTCD2962E561KR040M |
|  |  | 35*35 | 0.15 | 1.49 | 355 | 250 | RTCD2962E561KS035M |
|  | 680 | 30*45 | 0.15 | 1.71 | 295 | 210 | RTCD2962E681KR045M |
|  |  | 35*40 | 0.15 | 1.74 | 295 | 210 | RTCD2962E681KS040M |
|  | 820 | 30*50 | 0.15 | 1.94 | 245 | 175 | RTCD2962E821KR050M |
|  | 1000 | 35*45 | 0.15 | 2.21 | 200 | 140 | RTCD2962E102KS045M |
| 350 2V (400) | 68 | 22*25 | 0.20 | 0.34 | 3910 | 2735 | RTCD2962V680KP025M |
|  | 82 | 22*30 | 0.20 | 0.41 | 3240 | 2270 | RTCD2962V820KP030M |
|  | 100 | 25*25 | 0.20 | 0.47 | 2660 | 1860 | RTCD2962V101KQ025M |
|  | 120 | 22*35 | 0.20 | 0.52 | 2220 | 1550 | RTCD2962V121KP035M |
|  |  | 25*30 | 0.20 | 0.53 | 2220 | 1550 | RTCD2962V121KQ030M |
|  |  | 30*25 | 0.20 | 0.53 | 2220 | 1550 | RTCD2962V121KR025M |
|  | 150 | 22*40 | 0.20 | 0.59 | 1770 | 1240 | RTCD2962V151KP040M |
|  |  | 25*35 | 0.20 | 0.61 | 1770 | 1240 | RTCD2962V151KQ035M |
|  | 180 | 22*45 | 0.20 | 0.68 | 1480 | 1040 | RTCD2962V181KP045M |
|  |  | 25*40 | 0.20 | 0.71 | 1480 | 1040 | RTCD2962V181KQ040M |
|  |  | 30*30 | 0.20 | 0.71 | 1480 | 1040 | RTCD2962V181KR030M |
|  | 220 | 22*50 | 0.20 | 0.79 | 1210 | 850 | RTCD2962V221KP050M |
|  |  | 25*45 | 0.20 | 0.82 | 1210 | 850 | RTCD2962V221KQ045M |
|  |  | 30*35 | 0.20 | 0.82 | 1210 | 850 | RTCD2962V221KR035M |
|  | 270 | 25*50 | 0.20 | 0.94 | 1000 | 690 | RTCD2962V271KQ050M |
|  |  | 30*40 | 0.20 | 0.93 | 1000 | 690 | RTCD2962V271KR040M |
|  |  | 35*30 | 0.20 | 0.91 | 1000 | 690 | RTCD2962V271KS030M |
|  | 330 | 30*45 | 0.20 | 1.06 | 815 | 570 | RTCD2962V331KR045M |
|  |  | 35*35 | 0.20 | 1.02 | 815 | 570 | RTCD2962V331KS035M |
|  | 390 | 30*50 | 0.20 | 1.18 | 690 | 480 | RTCD2962V391KR050M |
|  |  | 35*40 | 0.20 | 1.14 | 690 | 480 | RTCD2962V391KS040M |
|  | 470 | 35*45 | 0.20 | 1.26 | 570 | 400 | RTCD2962V471KS045M |
|  | 560 | 35*50 | 0.20 | 1.40 | 480 | 350 | RTCD2962V561KS050M |
| 400 2G (450) | 68 | 22*30 | 0.20 | 0.38 | 3910 | 2735 | RTCD2962G680KP030M |
|  | 82 | 25*25 | 0.20 | 0.41 | 3240 | 2270 | RTCD2962G820KQ025M |
|  | 100 | 22*35 | 0.20 | 0.46 | 2660 | 1860 | RTCD2962G101KP035M |
|  |  | 25*30 | 0.20 | 0.48 | 2660 | 1860 | RTCD2962G101KQ030M |
|  |  | 30*25 | 0.20 | 0.48 | 2660 | 1860 | RTCD2962G101KR025M |
|  | 120 | 22*40 | 0.20 | 0.53 | 2220 | 1550 | RTCD2962G121KP040M |
|  |  | 25*35 | 0.20 | 0.55 | 2220 | 1550 | RTCD2962G121KQ035M |
|  |  | 30*30 | 0.20 | 0.56 | 2220 | 1550 | RTCD2962G121KR030M |
|  | 150 | 22*50 | 0.20 | 0.63 | 1770 | 1240 | RTCD2962G151KP050M |
|  |  | 25*40 | 0.20 | 0.65 | 1770 | 1240 | RTCD2962G151KQ040M |
|  | 180 | 25*45 | 0.20 | 0.72 | 1480 | 1035 | RTCD2962G181KQ045M |
|  |  | 30*35 | 0.20 | 0.74 | 1480 | 1035 | RTCD2962G181KR035M |
|  | 220 | 25*50 | 0.20 | 0.79 | 1210 | 850 | RTCD2962G221KQ050M |
|  |  | 30*40 | 0.20 | 0.85 | 1210 | 850 | RTCD2962G221KR040M |
|  |  | 35*30 | 0.20 | 0.89 | 1210 | 850 | RTCD2962G221KS030M |
|  | 270 | 30*45 | 0.20 | 0.98 | 985 | 690 | RTCD2962G271KR045M |
|  |  | 35*35 | 0.20 | 0.96 | 985 | 690 | RTCD2962G271KS035M |
|  | 330 | 30*50 | 0.20 | 1.12 | 810 | 570 | RTCD2962G331KR050M |
|  |  | 35*40 | 0.20 | 1.12 | 810 | 570 | RTCD2962G331KS040M |
|  | 390 | 35*45 | 0.20 | 1.27 | 690 | 480 | RTCD2962G391KS045M |
|  | 470 | 35*50 | 0.20 | 1.33 | 570 | 400 | RTCD2962G471KS050M |

| Rated Voltage code (V.DC) | Capacitance ( μF) | Case size ΦD×L(mm) | tanδ 20℃, 120Hz | Ripple current 105℃, 120Hz (Arms) | Max ESR 20℃, 120Hz (mΩ) | ESR(typ.) 20℃, 120Hz (mΩ) | Part number |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 450 2W (500) | 68 | 22*30 | 0.25 | 0.38 | 3910 | 2740 | RTCD2962W680KP030M |
|  | 82 | 22*35 | 0.25 | 0.44 | 3240 | 2270 | RTCD2962W820KP035M |
|  |  | 25*30 | 0.25 | 0.45 | 3240 | 2270 | RTCD2962W820KQ030M |
|  |  | 30*25 | 0.25 | 0.46 | 3240 | 2270 | RTCD2962W820KR025M |
|  | 100 | 22*40 | 0.25 | 0.50 | 2660 | 1860 | RTCD2962W101KP040M |
|  |  | 25*35 | 0.25 | 0.52 | 2660 | 1860 | RTCD2962W101KQ035M |
|  | 120 | 22*50 | 0.25 | 0.58 | 2220 | 1550 | RTCD2962W121KP050M |
|  |  | 25*40 | 0.25 | 0.58 | 2220 | 1550 | RTCD2962W121KQ040M |
|  |  | 30*30 | 0.25 | 0.58 | 2220 | 1550 | RTCD2962W121KR030M |
|  | 150 | 25*45 | 0.25 | 0.66 | 1770 | 1240 | RTCD2962W151KQ045M |
|  |  | 30*35 | 0.25 | 0.68 | 1770 | 1240 | RTCD2962W151KR035M |
|  | 180 | 25*50 | 0.25 | 0.74 | 1480 | 1035 | RTCD2962W181KQ050M |
|  |  | 30*40 | 0.25 | 0.77 | 1480 | 1035 | RTCD2962W181KR040M |
|  |  | 35*30 | 0.25 | 0.77 | 1480 | 1035 | RTCD2962W181KS030M |
|  | 220 | 30*45 | 0.25 | 0.88 | 1210 | 850 | RTCD2962W221KR045M |
|  |  | 35*35 | 0.25 | 0.88 | 1210 | 850 | RTCD2962W221KS035M |
|  | 270 | 30*50 | 0.25 | .0.99 | 990 | 690 | RTCD2962W271KR050M |
|  |  | 35*40 | 0.25 | 1.02 | 990 | 690 | RTCD2962W271KS040M |
|  | 330 | 35*45 | 0.25 | 1.15 | 810 | 570 | RTCD2962W331KS045M |
|  | 390 | 35*50 | 0.25 | 1.29 | 690 | 480 | RTCD2962W391KS050M |