RTCD289 SERIES　　　（ 85℃ 2000H）

- Compliant to the RoHS directive.

- Standard product,Load life of 2000 hours at 85℃.

- Used in switching power, frequency converter circuit,

filtering circuit, air conditioning, for welder and PCB mounting etc.

■Specification

| Item | Performance Characteristics |
| --- | --- |
| Operating range | -40℃～+85℃ | -25℃～+85℃ |
| Rated voltage range | 10V～250V | 315V～500V |
| Capacitance tolerance | ±20% (20℃, 120Hz) |
| Leakage current | I≤0.01CV(μA) or1.5mA (Whichever is smaller) (20℃, after 5 minutes) C=Nominal capacitance(μF), V=Rated voltage(V) |
| Dissipation factor (20℃，120Hz) | UR(V) 10～16 25～35 50 63 80～100 160～200 250～500 tanδ 0.45 0.35 0.30 0.25 0.20 0.15 0.15 |
| Stability at Low Temperature (Impedance ratio at120Hz) | UR(V) 10 16～100 160～200 250～400 450～500 Z(-25℃)/Z(+20℃) 5 4 3 4 Z(-40℃)/Z(+20℃) 18 15 10 8 — |
| Load Life | After applying rated voltage with specified ripple current for 2000 hours at 85℃(the peak voltage shall not exceed the rated voltage), and then restored for 24 hours, capacitor shall meet the following requirement: Capacitance change Within ±20% of the initial value. Dissipation factor Not more than 200% of the initial specified value. Leakage current Not more than the initial specified value. |
| Shelf Life | After storing for 1000 hours at 85℃,UR to be applied for 30 minutes and then restored for 24 hours, capacitor shall meet the following requirement: Capacitance change Within ±20% of the initial value. Dissipation factor Not more than 200% of the initial specified value. Leakage current Not more than the initial specified value. |
| Standard | JIS C 5101-4 |

■Coefficient of rated ripple current

| T (℃) UR(V) | 40 | 55 | 70 | 85 |  | F (Hz) UR(V) | 50(60) | 120 | 1K | 10K | 100K |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| <160 | 2.1 | 1.8 | 1.5 | 1.0 |  | ≤50 | 0.95 | 1.00 | 1.10 | 1.15 | 1.15 |
| ≥160 | 1.7 | 1.5 | 1.3 | 1.0 |  | 63-100 | 0.95 | 1.00 | 1.16 | 1.30 | 1.33 |
|  |  |  |  |  |  | ≥160 | 0.95 | 1.00 | 1.20 | 1.50 | 1.55 |

■Drawing                        Unit：mm

*:Shorter terminal is: 4.0±0.5mm

| Rated Voltage code (V.DC) | Capacitance( μF) | Case size ΦD×L(mm) | tanδ 20℃, 120Hz | Ripple current 85℃, 120Hz (Arms) | Max ESR 20℃, 120Hz (mΩ) | ESR(typ.) 20℃, 120Hz (mΩ) | Part number |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 10 1A (13) | 12000 | 22×30 | 0.45 | 3.30 | 50 | 40 | RTCD2891A123KP030M |
|  | 15000 | 25×25 | 0.45 | 3.31 | 40 | 30 | RTCD2891A153KQ025M |
|  | 18000 | 25×30 | 0.45 | 3.96 | 32 | 26 | RTCD2891A183KQ030M |
|  | 22000 | 25×35 | 0.45 | 4.41 | 25 | 20 | RTCD2891A223KQ035M |
|  | 33000 | 30×30 | 0.45 | 4.81 | 18 | 13 | RTCD2891A333KR030M |
|  | 39000 | 30×35 | 0.45 | 5.31 | 15 | 11 | RTCD2891A393KR035M |
|  | 47000 | 30×40 | 0.45 | 6.1 | 12 | 9.1 | RTCD2891A473KR040M |
|  | 68000 | 35×40 | 0.45 | 7.7 | 8 | 6.3 | RTCD2891A683KS040M |
|  | 82000 | 35×45 | 0.45 | 8.72 | 7 | 5.2 | RTCD2891A823KS045M |
| 16 1C (20) | 8200 | 22×25 | 0.45 | 2.22 | 66 | 51 | RTCD2891C822KP025M |
|  | 10000 | 22×30 | 0.45 | 2.66 | 55 | 42 | RTCD2891C103KP030M |
|  |  | 25×25 | 0.45 | 2.66 | 55 | 42 | RTCD2891C103KQ025M |
|  | 12000 | 22×35 | 0.45 | 2.99 | 48 | 35 | RTCD2891C123KP035M |
|  | 15000 | 22×40 | 0.45 | 3.33 | 38 | 30 | RTCD2891C153KP040M |
|  |  | 25×30 | 0.45 | 3.33 | 38 | 30 | RTCD2891C153KQ030M |
|  |  | 30×25 | 0.45 | 3.34 | 38 | 30 | RTCD2891C153KR025M |
|  | 18000 | 22×45 | 0.45 | 3.88 | 32 | 23 | RTCD2891C183KP045M |
|  |  | 25×35 | 0.45 | 3.87 | 32 | 23 | RTCD2891C183KQ035M |
|  | 22000 | 22×50 | 0.45 | 4.42 | 28 | 20 | RTCD2891C223KP050M |
|  |  | 25×40 | 0.45 | 4.42 | 28 | 20 | RTCD2891C223KQ040M |
|  |  | 30×30 | 0.45 | 4.42 | 28 | 20 | RTCD2891C223KR030M |
|  |  | 35×25 | 0.45 | 4.44 | 28 | 20 | RTCD2891C223KS025M |
| 25 1E (32) | 5600 | 22×25 | 0.35 | 2.20 | 85 | 66 | RTCD2891E562KP025M |
|  | 6800 | 22×30 | 0.35 | 2.33 | 70 | 55 | RTCD2891E682KP030M |
|  |  | 25×25 | 0.35 | 2.33 | 70 | 55 | RTCD2891E682KQ025M |
|  | 8200 | 22×35 | 0.35 | 2.66 | 58 | 48 | RTCD2891E822KP035M |
|  | 10000 | 22×40 | 0.35 | 2.99 | 50 | 40 | RTCD2891E103KP040M |
|  |  | 25×30 | 0.35 | 2.88 | 50 | 40 | RTCD2891E103KQ030M |
|  |  | 30×25 | 0.35 | 2.88 | 50 | 40 | RTCD2891E103KR025M |
|  | 12000 | 22×45 | 0.35 | 3.33 | 40 | 31 | RTCD2891E123KP045M |
|  |  | 25×35 | 0.35 | 3.32 | 40 | 31 | RTCD2891E123KQ035M |
|  |  | 30×30 | 0.35 | 3.40 | 40 | 31 | RTCD2891E123KR030M |
|  | 15000 | 25×40 | 0.35 | 3.77 | 35 | 25 | RTCD2891E153KQ040M |
|  |  | 30×30 | 0.35 | 3.80 | 35 | 25 | RTCD2891E153KR030M |
|  |  | 35×25 | 0.35 | 3.90 | 35 | 25 | RTCD2891E153KS025M |
|  | 18000 | 25×50 | 0.35 | 4.35 | 30 | 21 | RTCD2891E183KQ050M |
|  |  | 30×35 | 0.35 | 4.32 | 30 | 21 | RTCD2891E183KR035M |
|  |  | 35×30 | 0.35 | 4.30 | 30 | 21 | RTCD2891E183KS030M |
|  | 22000 | 30×40 | 0.35 | 4.90 | 25 | 18 | RTCD2891E223KR040M |
|  |  | 35×35 | 0.35 | 5.00 | 25 | 18 | RTCD2891E223KS035M |
| 35 1V (44) | 3300 | 22×25 | 0.35 | 1.88 | 100 | 82 | RTCD2891V332KP025M |
|  | 3900 | 22×30 | 0.35 | 2.11 | 90 | 70 | RTCD2891V392KP030M |
|  | 4700 | 25×25 | 0.35 | 2.20 | 75 | 60 | RTCD2891V472KQ025M |
|  | 5600 | 22×35 | 0.35 | 2.33 | 75 | 60 | RTCD2891V562KP035M |
|  |  | 25×30 | 0.35 | 2.33 | 75 | 60 | RTCD2891V562KQ030M |
|  | 6800 | 22×40 | 0.35 | 2.99 | 60 | 50 | RTCD2891V682KP040M |
|  |  | 25×35 | 0.35 | 2.70 | 60 | 50 | RTCD2891V682KQ035M |
|  |  | 30×25 | 0.35 | 2.77 | 60 | 50 | RTCD2891V682KR025M |
|  | 8200 | 22×50 | 0.35 | 2.85 | 58 | 47 | RTCD2891V822KP050M |
|  |  | 25×40 | 0.35 | 2.85 | 58 | 47 | RTCD2891V822KQ040M |
|  |  | 30×30 | 0.35 | 2.85 | 58 | 47 | RTCD2891V822KR030M |
|  |  | 35×25 | 0.35 | 2.90 | 58 | 47 | RTCD2891V822KS025M |
|  | 10000 | 25×45 | 0.35 | 3.20 | 50 | 40 | RTCD2891V103KQ045M |
|  |  | 30×35 3…3 | 0.35 | 3.30 | 50 | 40 | RTCD2891V103KR035M |
|  | 12000 | 25×50 | 0.35 | 3.58 | 40 | 31 | RTCD2891V123KQ050M |
|  |  | 30×40 | 0.35 | 3.58 | 40 | 31 | RTCD2891V123KR040M |
|  |  | 35×30 | 0.35 | 3.66 | 40 | 31 | RTCD2891V123KS030M |
|  | 15000 | 30×45 | 0.35 | 4.20 | 35 | 25 | RTCD2891V153KR045M |
|  |  | 35×35 | 0.35 | 4.20 | 35 | 25 | RTCD2891V153KS035M |
|  | 18000 | 30×50 | 0.35 | 4.70 | 30 | 22 | RTCD2891V183KR050M |
|  |  | 35×40 | 0.35 | 4.70 | 30 | 22 | RTCD2891V183KS040M |
|  | 22000 | 35×45 | 0.35 | 5.40 | 25 | 18 | RTCD2891V223KS045M |

■RTCD289 Dimensions

| Rated Voltage code (V.DC) | Capacitance( μF) | Case size ΦD×L(mm) | tanδ 20℃, 120Hz | Ripple current 85℃, 120Hz (Arms) | Max ESR 20℃, 120Hz (mΩ) | ESR(typ.) 20℃, 120Hz (mΩ) | Part number |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 50 1H (63) | 2200 | 22×25 | 0.30 | 1.80 | 120 | 100 | RTCD2891H222KP025M |
|  | 2700 | 22*30 | 0.30 | 1.95 | 105 | 80 | RTCD2891H272KP030M |
|  |  | 25*25 | 0.30 | 1.90 | 105 | 80 | RTCD2891H272KQ025M |
|  | 3300 | 22*35 | 0.30 | 2.20 | 105 | 81 | RTCD2891H332KP035M |
|  |  | 25*30 | 0.30 | 2.10 | 105 | 81 | RTCD2891H332KQ030M |
|  | 3900 | 25*35 | 0.30 | 2.31 | 90 | 70 | RTCD2891H392KQ035M |
|  |  | 30*25 | 0.30 | 2.30 | 90 | 70 | RTCD2891H392KR025M |
|  | 4700 | 22*40 | 0.30 | 2.54 | 75 | 60 | RTCD2891H472KP040M |
|  |  | 25*35 | 0.30 | 2.54 | 75 | 60 | RTCD2891H472KQ035M |
|  | 5600 | 25*40 | 0.30 | 2.58 | 75 | 60 | RTCD2891H562KQ040M |
|  |  | 30*30 | 0.30 | 2.54 | 75 | 60 | RTCD2891H562KR030M |
|  | 6800 | 25*45 | 0.30 | 2.83 | 60 | 50 | RTCD2891H682KQ045M |
|  |  | 30*35 | 0.30 | 2.80 | 60 | 50 | RTCD2891H682KR035M |
|  | 8200 | 25*50 | 0.30 | 3.50 | 60 | 50 | RTCD2891H822KQ050M |
|  |  | 30*40 | 0.30 | 3.20 | 60 | 50 | RTCD2891H822KR040M |
|  | 10000 | 30*45 | 0.30 | 3.60 | 50 | 40 | RTCD2891H103KR045M |
|  |  | 35*35 | 0.30 | 3.60 | 50 | 40 | RTCD2891H103KS035M |
|  | 12000 | 30*50 | 0.30 | 4.00 | 40 | 31 | RTCD2891H123KR050M |
|  |  | 35*40 | 0.30 | 3.90 | 40 | 31 | RTCD2891H123KS040M |
|  | 15000 | 35*50 | 0.30 | 4.55 | 40 | 30 | RTCD2891H153KS050M |
|  | 22000 | 35*60 | 0.30 | 5.96 | 40 | 30 | RTCD2891H223KS060M |
| 63 1J (79) | 1500 | 22*25 | 0.25 | 1.62 | 140 | 110 | RTCD2891J152KP025M |
|  | 1800 | 22*30 | 0.25 | 1.93 | 115 | 90 | RTCD2891J182KP030M |
|  | 2200 | 22*30 | 0.25 | 2.10 | 100 | 75 | RTCD2891J222KP030M |
|  |  | 25*25 | 0.25 | 2.05 | 100 | 75 | RTCD2891J222KQ025M |
|  | 2700 | 22*35 | 0.25 | 2.25 | 80 | 60 | RTCD2891J272KP035M |
|  |  | 25*30 | 0.25 | 2.33 | 80 | 60 | RTCD2891J272KQ030M |
|  | 3300 | 22*40 | 0.25 | 2.37 | 90 | 68 | RTCD2891J332KP040M |
|  |  | 25*35 | 0.25 | 2.36 | 90 | 68 | RTCD2891J332KQ035M |
|  |  | 30*25 | 0.25 | 2.31 | 90 | 68 | RTCD2891J332KR025M |
|  | 3900 | 22*45 | 0.25 | 2.52 | 70 | 60 | RTCD2891J392KP045M |
|  |  | 25*40 | 0.25 | 2.60 | 70 | 60 | RTCD2891J392KQ040M |
|  |  | 30*30 | 0.25 | 2.51 | 70 | 60 | RTCD2891J392KR030M |
|  | 4700 | 22*50 | 0.25 | 2.91 | 65 | 52 | RTCD2891J472KP050M |
|  |  | 25*45 | 0.25 | 3.04 | 65 | 52 | RTCD2891J472KQ045M |
|  | 5600 | 25*45 | 0.25 | 3.14 | 50 | 40 | RTCD2891J562KQ045M |
|  |  | 30*35 | 0.25 | 3.22 | 50 | 40 | RTCD2891J562KR035M |
|  |  | 35*30 | 0.25 | 3.30 | 50 | 40 | RTCD2891J562KS030M |
|  | 6800 | 30*40 | 0.25 | 3.60 | 45 | 35 | RTCD2891J682KR040M |
|  |  | 35*35 | 0.25 | 3.72 | 45 | 35 | RTCD2891J682KS035M |
|  | 8200 | 30*50 | 0.25 | 3.70 | 45 | 35 | RTCD2891J822KR050M |
|  |  | 35*40 | 0.25 | 3.80 | 45 | 35 | RTCD2891J822KS040M |
|  | 10000 | 35*45 | 0.25 | 4.32 | 35 | 30 | RTCD2891J103KS045M |
|  | 12000 | 35*50 | 0.25 | 4.81 | 30 | 25 | RTCD2891J123KS050M |
| 80 1K (100) | 1000 | 22*25 | 0.20 | 1.30 | 200 | 160 | RTCD2891K102KP025M |
|  | 1200 | 22*30 | 0.20 | 1.50 | 170 | 135 | RTCD2891K122KP030M |
|  |  | 22*40 | 0.20 | 1.70 | 170 | 135 | RTCD2891K122KP040M |
|  | 1500 | 22*35 | 0.20 | 1.82 | 135 | 110 | RTCD2891K152KP035M |
|  |  | 25*25 | 0.20 | 1.70 | 135 | 110 | RTCD2891K152KQ025M |
|  | 1800 | 22*35 | 0.20 | 1.94 | 115 | 90 | RTCD2891K182KP035M |
|  |  | 25*30 | 0.20 | 1.91 | 115 | 90 | RTCD2891K182KQ030M |
|  | 2200 | 22*40 | 0.20 | 2.14 | 95 | 75 | RTCD2891K222KP040M |
|  |  | 25*35 | 0.20 | 2.25 | 95 | 75 | RTCD2891K222KQ035M |
|  |  | 30*25 | 0.20 | 2.23 | 95 | 75 | RTCD2891K222KR025M |
|  | 2700 | 22*50 | 0.20 | 2.56 | 75 | 60 | RTCD2891K272KP050M |
|  |  | 25*40 | 0.20 | 2.53 | 75 | 60 | RTCD2891K272KQ040M |
|  |  | 30*30 | 0.20 | 2.50 | 75 | 60 | RTCD2891K272KR030M |
|  | 3300 | 25*45 | 0.20 | 2.84 | 65 | 50 | RTCD2891K332KQ045M |
|  |  | 30*35 | 0.20 | 2.81 | 65 | 50 | RTCD2891K332KR035M |
|  | 3900 | 30*40 | 0.20 | 3.22 | 55 | 45 | RTCD2891K392KR040M |
|  |  | 35*30 | 0.20 | 3.20 | 55 | 45 | RTCD2891K392KS030M |
|  | 4700 | 30*45 | 0.20 | 3.66 | 45 | 40 | RTCD2891K472KR045M |
|  |  | 35*35 | 0.20 | 3.62 | 45 | 40 | RTCD2891K472KS035M |
|  | 5600 | 30*50 | 0.20 | 3.52 | 50 | 40 | RTCD2891K562KR050M |
|  |  | 35*40 | 0.20 | 3.51 | 50 | 40 | RTCD2891K562KS040M |

| Rated Voltage code (V.DC) | Capacitance ( μF) | Case size ΦD×L(mm) | tanδ 20℃, 120Hz | Ripple current 85℃, 120Hz (Arms) | Max ESR 20℃, 120Hz (mΩ) | ESR(typ.) 20℃, 120Hz (mΩ) | Part number |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 80 1K (100) | 6800 | 35*50 | 0.20 | 4.10 | 45 | 35 | RTCD2891K682KS050M |
|  | 10000 | 40*65 | 0.2 | 6.0 | 45 | 32 | RTCD2891K103KV060M |
| 100 2A (125) | 680 | 22*25 | 0.20 | 1.10 | 300 | 240 | RTCD2892A681KP025M |
|  | 820 | 22*30 | 0.20 | 1.21 | 250 | 200 | RTCD2892A821KP030M |
|  | 1000 | 22*30 | 0.20 | 1.43 | 210 | 165 | RTCD2892A102KP030M |
|  |  | 22*35 | 0.20 | 1.53 | 210 | 165 | RTCD2892A102KP035M |
|  |  | 25*25 | 0.20 | 1.45 | 210 | 165 | RTCD2892A102KQ025M |
|  | 1200 | 22*35 | 0.20 | 1.63 | 180 | 145 | RTCD2892A122KP035M |
|  |  | 25*30 | 0.20 | 1.61 | 180 | 145 | RTCD2892A122KQ030M |
|  | 1500 | 22*40 | 0.20 | 1.81 | 140 | 115 | RTCD2892A152KP040M |
|  |  | 25*35 | 0.20 | 1.72 | 140 | 115 | RTCD2892A152KQ035M |
|  |  | 30*25 | 0.20 | 1.83 | 140 | 115 | RTCD2892A152KR025M |
|  | 1800 | 22*50 | 0.20 | 2.15 | 120 | 95 | RTCD2892A182KP050M |
|  |  | 25*40 | 0.20 | 2.12 | 120 | 95 | RTCD2892A182KQ040M |
|  |  | 30*30 | 0.20 | 2.10 | 120 | 95 | RTCD2892A182KR030M |
|  | 2200 | 25*45 | 0.20 | 2.23 | 100 | 80 | RTCD2892A222KQ045M |
|  |  | 30*35 | 0.20 | 2.32 | 100 | 80 | RTCD2892A222KR035M |
|  |  | 35*30 | 0.20 | 2.51 | 100 | 80 | RTCD2892A222KS030M |
|  | 2700 | 25*50 | 0.20 | 2.62 | 80 | 65 | RTCD2892A272KQ050M |
|  |  | 30*40 | 0.20 | 2.70 | 80 | 65 | RTCD2892A272KR040M |
|  | 3300 | 30*45 | 0.20 | 3.10 | 70 | 55 | RTCD2892A332KR045M |
|  |  | 35*35 | 0.20 | 3.05 | 70 | 55 | RTCD2892A332KS035M |
|  | 3900 | 30*50 | 0.20 | 3.44 | 60 | 45 | RTCD2892A392KR050M |
|  |  | 35*40 | 0.20 | 3.42 | 60 | 45 | RTCD2892A392KS040M |
|  | 4700 | 35*50 | 0.20 | 4.03 | 50 | 40 | RTCD2892A472KS050M |
| 160 2C (200) | 270 | 22*25 | 0.15 | 1.20 | 500 | 400 | RTCD2892C271KP025M |
|  | 330 | 22*30 | 0.15 | 1.31 | 420 | 350 | RTCD2892C331KP030M |
|  | 390 | 22*35 | 0.15 | 1.54 | 350 | 280 | RTCD2892C391KP035M |
|  |  | 25*25 | 0.15 | 1.52 | 350 | 280 | RTCD2892C391KQ025M |
|  | 470 | 25*30 | 0.15 | 1.62 | 300 | 230 | RTCD2892C471KQ030M |
|  | 560 | 22*35 | 0.15 | 1.92 | 250 | 195 | RTCD2892C561KP035M |
|  |  | 25*30 | 0.15 | 1.91 | 250 | 195 | RTCD2892C561KQ030M |
|  |  | 30*25 | 0.15 | 2.00 | 250 | 195 | RTCD2892C561KR025M |
|  | 680 | 22*40 | 0.15 | 2.11 | 200 | 160 | RTCD2892C681KP040M |
|  |  | 25*35 | 0.15 | 2.20 | 200 | 160 | RTCD2892C681KQ035M |
|  | 820 | 22*50 | 0.15 | 2.51 | 170 | 135 | RTCD2892C821KP050M |
|  |  | 25*45 | 0.15 | 2.43 | 170 | 135 | RTCD2892C821KQ045M |
|  |  | 30*30 | 0.15 | 2.50 | 170 | 135 | RTCD2892C821KR030M |
|  | 1000 | 25*45 | 0.15 | 2.70 | 140 | 110 | RTCD2892C102KQ045M |
|  |  | 30*40 | 0.15 | 2.81 | 140 | 110 | RTCD2892C102KR040M |
|  |  | 35*35 | 0.15 | 2.70 | 140 | 110 | RTCD2892C102KS035M |
|  | 1200 | 30*40 | 0.15 | 3.21 | 120 | 92 | RTCD2892C122KR040M |
|  |  | 35*35 | 0.15 | 3.13 | 120 | 92 | RTCD2892C122KS035M |
|  | 1500 | 30*45 | 0.15 | 3.72 | 110 | 90 | RTCD2892C152KR045M |
|  |  | 35*40 | 0.15 | 3.53 | 110 | 90 | RTCD2892C152KS040M |
|  | 1800 | 35*45 | 0.15 | 3.93 | 90 | 75 | RTCD2892C182KS045M |
|  | 2200 | 35*50 | 0.15 | 4.51 | 80 | 60 | RTCD2892C222KS050M |
| 180 2K (225) | 270 | 22*25 | 0.15 | 1.21 | 500 | 400 | RTCD2892K271KP025M |
|  | 330 | 22*30 | 0.15 | 1.41 | 400 | 330 | RTCD2892K331KP030M |
|  | 390 | 25*25 | 0.15 | 1.52 | 350 | 280 | RTCD2892K391KQ025M |
|  | 470 | 22*35 | 0.15 | 1.71 | 285 | 230 | RTCD2892K471KP035M |
|  |  | 25*30 | 0.15 | 1.72 | 285 | 230 | RTCD2892K471KQ030M |
|  |  | 30*25 | 0.15 | 1.82 | 285 | 230 | RTCD2892K471KR025M |
|  | 560 | 22*40 | 0.15 | 1.95 | 240 | 200 | RTCD2892K561KP040M |
|  |  | 25*35 | 0.15 | 2.01 | 240 | 200 | RTCD2892K561KQ035M |
|  | 680 | 22*50 | 0.15 | 2.22 | 200 | 160 | RTCD2892K681KP050M |
|  |  | 25*40 | 0.15 | 2.22 | 200 | 160 | RTCD2892K681KQ040M |
|  |  | 30*30 | 0.15 | 2.30 | 200 | 160 | RTCD2892K681KR030M |
|  |  | 35*25 | 0.15 | 2.21 | 240 | 190 | RTCD2892K681KS025M |
|  | 820 | 25*45 | 0.15 | 2.52 | 170 | 130 | RTCD2892K821KQ045M |
|  |  | 30*35 | 0.15 | 2.61 | 170 | 130 | RTCD2892K821KR035M |
|  |  | 35*30 | 0.15 | 2.50 | 200 | 160 | RTCD2892K821KS030M |
|  | 1000 | 25*50 | 0.15 | 2.90 | 140 | 110 | RTCD2892K102KQ050M |
|  |  | 30*40 | 0.15 | 2.90 | 140 | 110 | RTCD2892K102KR040M |

| Rated Voltage code (V.DC) | Capacitance( μF) | Case size ΦD×L(mm) | tanδ 20℃, 120Hz | Ripple current 85℃, 120Hz (Arms) | Max ESR 20℃, 120Hz (mΩ) | ESR(typ.) 20℃, 120Hz (mΩ) | Part number |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 180 2K (225) | 1200 | 30*45 | 0.15 | 3.31 | 140 | 90 | RTCD2892K122KR045M |
|  |  | 35*35 | 0.15 | 3.12 | 140 | 110 | RTCD2892K122KS035M |
|  | 1500 | 35*45 | 0.15 | 3.61 | 110 | 90 | RTCD2892K152KS045M |
|  | 1800 | 35*50 | 0.15 | 4.12 | 90 | 80 | RTCD2892K182KS050M |
| 200 2D (250) | 220 | 22*25 | 0.15 | 1.10 | 600 | 500 | RTCD2892D221KP025M |
|  | 270 | 22*30 | 0.15 | 1.21 | 500 | 400 | RTCD2892D271KP030M |
|  | 330 | 22*30 | 0.15 | 1.41 | 410 | 330 | RTCD2892D331KP030M |
|  |  | 25*25 | 0.15 | 1.40 | 410 | 330 | RTCD2892D331KQ025M |
|  | 390 | 22*35 | 0.15 | 1.61 | 350 | 280 | RTCD2892D391KP035M |
|  |  | 25*30 | 0.15 | 1.61 | 350 | 280 | RTCD2892D391KQ030M |
|  | 470 | 22*40 | 0.15 | 1.81 | 300 | 230 | RTCD2892D471KP040M |
|  |  | 30*25 | 0.15 | 1.92 | 300 | 230 | RTCD2892D471KR025M |
|  | 560 | 22*45 | 0.15 | 2.03 | 250 | 200 | RTCD2892D561KP045M |
|  |  | 25*35 | 0.15 | 2.02 | 250 | 200 | RTCD2892D561KQ035M |
|  |  | 30*30 | 0.15 | 2.10 | 250 | 200 | RTCD2892D561KR030M |
|  |  | 35*25 | 0.15 | 2.02 | 250 | 200 | RTCD2892D561KS025M |
|  | 680 | 25*40 | 0.15 | 2.31 | 200 | 160 | RTCD2892D681KQ040M |
|  |  | 30*35 | 0.15 | 2.42 | 200 | 160 | RTCD2892D681KR035M |
|  | 820 | 25*50 | 0.15 | 2.61 | 170 | 135 | RTCD2892D821KQ050M |
|  |  | 30*40 | 0.15 | 2.71 | 170 | 135 | RTCD2892D821KR040M |
|  |  | 35*30 | 0.15 | 25.26 | 170 | 135 | RTCD2892D821KS030M |
|  | 1000 | 30*45 | 0.15 | 3.12 | 150 | 110 | RTCD2892D102KR045M |
|  |  | 35*35 | 0.15 | 2.83 | 160 | 130 | RTCD2892D102KS035M |
|  | 1200 | 30*50 | 0.15 | 3.42 | 120 | 90 | RTCD2892D122KR050M |
|  |  | 35*40 | 0.15 | 3.20 | 140 | 110 | RTCD2892D122KS040M |
|  | 1500 | 35*50 | 0.15 | 3.83 | 110 | 90 | RTCD2892D152KS050M |
| 250 2E (300) | 180 | 22*25 | 0.15 | 0.94 | 1110 | 890 | RTCD2892E181KP025M |
|  | 220 | 22*30 | 0.15 | 1.12 | 910 | 730 | RTCD2892E221KP030M |
|  |  | 25*25 | 0.15 | 1.13 | 910 | 730 | RTCD2892E221KQ025M |
|  | 270 | 22*35 | 0.15 | 1.23 | 750 | 600 | RTCD2892E271KP035M |
|  | 330 | 22*40 | 0.15 | 1.45 | 610 | 490 | RTCD2892E331KP040M |
|  |  | 25*30 | 0.15 | 1.43 | 610 | 490 | RTCD2892E331KQ030M |
|  |  | 25*35 | 0.15 | 1.52 | 610 | 490 | RTCD2892E331KQ035M |
|  |  | 30*25 | 0.15 | 1.53 | 610 | 490 | RTCD2892E331KR025M |
|  | 390 | 22*45 | 0.15 | 1.63 | 520 | 410 | RTCD2892E391KP045M |
|  |  | 25*35 | 0.15 | 1.62 | 520 | 410 | RTCD2892E391KQ035M |
|  | 470 | 25*40 | 0.15 | 1.83 | 430 | 340 | RTCD2892E471KQ040M |
|  |  | 30*30 | 0.15 | 1.82 | 430 | 340 | RTCD2892E471KR030M |
|  |  | 35*25 | 0.15 | 2.42 | 430 | 340 | RTCD2892E471KS025M |
|  | 560 | 25*45 | 0.15 | 2.05 | 360 | 290 | RTCD2892E561KQ045M |
|  |  | 30*35 | 0.15 | 2.05 | 360 | 290 | RTCD2892E561KR035M |
|  | 680 | 30*40 | 0.15 | 2.35 | 300 | 240 | RTCD2892E681KR040M |
|  |  | 35*30 | 0.15 | 2.63 | 300 | 240 | RTCD2892E681KS030M |
|  | 820 | 30*45 | 0.15 | 2.61 | 250 | 200 | RTCD2892E821KR045M |
|  |  | 35*35 | 0.15 | 2.60 | 250 | 200 | RTCD2892E821KS035M |
|  | 1000 | 35*40 | 0.15 | 3.02 | 200 | 165 | RTCD2892E102KS040M |
|  | 1200 | 35*45 | 0.15 | 3.43 | 170 | 140 | RTCD2892E122KS045M |
| 315 2F (365) | 100 | 22*25 | 0.15 | 0.67 | 2000 | 1600 | RTCD2892F101KP025M |
|  | 120 | 22*25 | 0.15 | 0.74 | 2000 | 1600 | RTCD2892F121KP025M |
|  | 150 | 22*30 | 0.15 | 0.86 | 1330 | 1100 | RTCD2892F151KP030M |
|  |  | 25*25 | 0.15 | 0.85 | 1330 | 1100 | RTCD2892F151KQ025M |
|  | 180 | 22*35 | 0.15 | 0.97 | 1110 | 890 | RTCD2892F181KP035M |
|  |  | 25*30 | 0.15 | 0.96 | 1110 | 890 | RTCD2892F181KQ030M |
|  | 220 | 22*40 | 0.15 | 1.14 | 910 | 730 | RTCD2892F221KP040M |
|  |  | 25*35 | 0.15 | 1.13 | 910 | 730 | RTCD2892F221KQ035M |
|  |  | 30*25 | 0.15 | 1.11 | 910 | 730 | RTCD2892F221KR025M |
|  | 270 | 22*45 | 0.15 | 1.23 | 740 | 600 | RTCD2892F271KP045M |
|  |  | 25*40 | 0.15 | 1.32 | 740 | 600 | RTCD2892F271KQ040M |
|  |  | 30*30 | 0.15 | 1.31 | 740 | 600 | RTCD2892F271KR030M |
|  |  | 35*25 | 0.15 | 1.30 | 740 | 600 | RTCD2892F271KS025M |
|  | 330 | 25*45 | 0.15 | 1.42 | 610 | 490 | RTCD2892F331KQ045M |
|  |  | 30*35 | 0.15 | 1.41 | 610 | 490 | RTCD2892F331KR035M |
|  | 390 | 30*40 | 0.15 | 1.62 | 520 | 410 | RTCD2892F391KR040M |
|  |  | 35*30 | 0.15 | 1.60 | 520 | 410 | RTCD2892F391KS030M |
|  | 470 | 30*45 | 0.15 | 1.81 | 430 | 345 | RTCD2892F471KR045M |
|  |  | 35*35 | 0.15 | 1.81 | 430 | 345 | RTCD2892F471KS035M |

| Rated Voltage code (V.DC) | Capacitance( μF) | Case size ΦD×L(mm) | tanδ 20℃, 120Hz | Ripple current 85℃, 120Hz (Arms) | Max ESR 20℃, 120Hz (mΩ) | ESR(typ.) 20℃, 120Hz (mΩ) | Part number |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 315 2F (365) | 560 | 30*50 | 0.15 | 2.04 | 360 | 290 | RTCD2892F561KR050M |
|  |  | 35*40 | 0.15 | 2.02 | 360 | 290 | RTCD2892F561KS040M |
|  | 680 | 35*45 | 0.15 | 2.30 | 300 | 240 | RTCD2892F681KS045M |
| 350 2V (400) | 82 | 22*25 | 0.15 | 0.65 | 2450 | 1950 | RTCD2892V820KP025M |
|  | 100 | 22*25 | 0.15 | 0.78 | 2000 | 1600 | RTCD2892V101KP025M |
|  | 120 | 22*30 | 0.15 | 0.84 | 1670 | 1330 | RTCD2892V121KP030M |
|  |  | 25*25 | 0.15 | 0.82 | 1670 | 1330 | RTCD2892V121KQ025M |
|  | 150 | 22*35 | 0.15 | 0.96 | 1330 | 1070 | RTCD2892V151KP035M |
|  |  | 25*30 | 0.15 | 0.95 | 1330 | 1070 | RTCD2892V151KQ030M |
|  | 180 | 22*40 | 0.15 | 1.15 | 1110 | 890 | RTCD2892V181KP040M |
|  |  | 30*25 | 0.15 | 0.12 | 1110 | 890 | RTCD2892V181KR025M |
|  | 220 | 22*45 | 0.15 | 1.24 | 920 | 730 | RTCD2892V221KP045M |
|  |  | 25*35 | 0.15 | 1.23 | 920 | 730 | RTCD2892V221KQ035M |
|  |  | 30*30 | 0.15 | 1.22 | 920 | 730 | RTCD2892V221KR030M |
|  | 270 | 25*45 | 0.15 | 1.44 | 745 | 595 | RTCD2892V271KQ045M |
|  |  | 30*35 | 0.15 | 1.43 | 745 | 595 | RTCD2892V271KR035M |
|  |  | 35*30 | 0.15 | 1.43 | 745 | 595 | RTCD2892V271KS030M |
|  | 330 | 25*50 | 0.15 | 1.65 | 610 | 485 | RTCD2892V331KQ050M |
|  |  | 30*40 | 0.15 | 1.65 | 610 | 485 | RTCD2892V331KR040M |
|  |  | 35*30 | 0.15 | 1.63 | 610 | 485 | RTCD2892V331KS030M |
|  | 390 | 30*40 | 0.15 | 1.74 | 515 | 410 | RTCD2892V391KR040M |
|  |  | 35*35 | 0.15 | 1.80 | 515 | 410 | RTCD2892V391KS035M |
|  | 470 | 30*45 | 0.15 | 2.05 | 430 | 340 | RTCD2892V471KR045M |
|  |  | 35*40 | 0.15 | 2.00 | 430 | 340 | RTCD2892V471KS040M |
|  | 560 | 35*45 | 0.15 | 2.31 | 360 | 290 | RTCD2892V561KS045M |
|  | 680 | 35*50 | 0.15 | 2.62 | 360 | 290 | RTCD2892V681KS050M |
|  | 820 | 35*60 | 0.15 | 2.82 | 250 | 200 | RTCD2892V821KS060M |
| 400 2G (450) | 82 | 22*25 | 0.15 | 0.64 | 2430 | 1945 | RTCD2892G820KP025M |
|  | 100 | 22*30 | 0.15 | 0.71 | 1995 | 1595 | RTCD2892G101KP030M |
|  |  | 25*25 | 0.15 | 0.70 | 1995 | 1595 | RTCD2892G101KQ025M |
|  | 120 | 22*35 | 0.15 | 0.80 | 1660 | 1330 | RTCD2892G121KP035M |
|  | 150 | 25*30 | 0.15 | 0.92 | 1330 | 1065 | RTCD2892G151KQ030M |
|  |  | 30*25 | 0.15 | 0.95 | 1330 | 1065 | RTCD2892G151KR025M |
|  | 180 | 25*35 | 0.15 | 1.01 | 1110 | 890 | RTCD2892G181KQ035M |
|  |  | 30*30 | 0.15 | 1.10 | 1110 | 890 | RTCD2892G181KR030M |
|  |  | 35*25 | 0.15 | 1.21 | 1110 | 890 | RTCD2892G181KS025M |
|  | 220 | 22*50 | 0.15 | 1.12 | 910 | 730 | RTCD2892G221KP050M |
|  |  | 25*40 | 0.15 | 1.23 | 910 | 730 | RTCD2892G221KQ040M |
|  |  | 30*35 | 0.15 | 1.24 | 910 | 730 | RTCD2892G221KR035M |
|  | 270 | 25*45 | 0.15 | 1.35 | 740 | 600 | RTCD2892G271KQ045M |
|  |  | 30*40 | 0.15 | 1.51 | 740 | 600 | RTCD2892G271KR040M |
|  |  | 35*35 | 0.15 | 1.56 | 740 | 600 | RTCD2892G271KS035M |
|  | 330 | 30*40 | 0.15 | 1.62 | 610 | 490 | RTCD2892G331KR040M |
|  |  | 30*45 | 0.15 | 1.71 | 610 | 490 | RTCD2892G331KR045M |
|  |  | 35*30 | 0.15 | 1.63 | 610 | 490 | RTCD2892G331KS030M |
|  | 390 | 30*50 | 0.15 | 1.83 | 515 | 415 | RTCD2892G391KR050M |
|  |  | 35*35 | 0.15 | 1.83 | 515 | 415 | RTCD2892G391KS035M |
|  | 470 | 35*40 | 0.15 | 2.04 | 425 | 345 | RTCD2892G471KS040M |
|  |  | 35*45 | 0.15 | 2.15 | 425 | 345 | RTCD2892G471KS045M |
|  |  | 35*50 | 0.15 | 2.40 | 425 | 345 | RTCD2892G471KS050M |
|  | 560 | 35*45 | 0.15 | 2.10 | 360 | 290 | RTCD2892G561KS045M |
|  |  | 35*50 | 0.15 | 2.30 | 360 | 290 | RTCD2892G561KS050M |
|  | 680 | 35*50 | 0.15 | 2.36 | 350 | 270 | RTCD2892G681KS050M |
|  | 820 | 35*60 | 0.15 | 3.00 | 342 | 260 | RTCD2892G821KS060M |
|  | 1000 | 35*65 | 0.15 | 3.10 | 300 | 250 | RTCD2892G102KS065M |
|  | 1200 | 35*80 | 0.15 | 3.70 | 300 | 250 | RTCD2892G122KS080M |
| 450 2W (500) | 68 | 22*30 | 0.15 | 0.57 | 2930 | 2345 | RTCD2892W680KP030M |
|  | 82 | 25*35 | 0.15 | 0.70 | 2430 | 1945 | RTCD2892W820KQ035M |
|  | 100 | 22*35 | 0.15 | 0.72 | 1995 | 1600 | RTCD2892W101KP035M |
|  |  | 25*30 | 0.15 | 0.73 | 1995 | 1600 | RTCD2892W101KQ030M |
|  | 120 | 22*40 | 0.15 | 0.80 | 1660 | 1330 | RTCD2892W121KP040M |
|  |  | 25*35 | 0.15 | 0.84 | 1660 | 1330 | RTCD2892W121KQ035M |

| Rated Voltage code (V.DC) | Capacitance( μF) | Case size ΦD×L(mm) | tanδ 20℃, 120Hz | Ripple current 85℃, 120Hz (Arms) | Max ESR 20℃, 120Hz (mΩ) | ESR(typ.) 20℃, 120Hz (mΩ) | Part number |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 450 2W (500) | 150 | 25*40 | 0.15 | 0.95 | 1330 | 1070 | RTCD2892W151KQ040M |
|  |  | 30*30 | 0.15 | 0.96 | 1330 | 1070 | RTCD2892W151KR030M |
|  |  | 35*25 | 0.15 | 0.99 | 1330 | 1070 | RTCD2892W151KS025M |
|  | 180 | 25*45 | 0.15 | 1.10 | 1110 | 895 | RTCD2892W181KQ045M |
|  |  | 30*35 | 0.15 | 1.11 | 1110 | 895 | RTCD2892W181KR035M |
|  |  | 35*25 | 0.15 | 1.23 | 1110 | 895 | RTCD2892W181KS025M |
|  | 220 | 25*50 | 0.15 | 1.20 | 915 | 730 | RTCD2892W221KQ050M |
|  |  | 30*40 | 0.15 | 1.32 | 915 | 730 | RTCD2892W221KR040M |
|  |  | 35*30 | 0.15 | 1.32 | 915 | 730 | RTCD2892W221KS030M |
|  | 270 | 30*45 | 0.15 | 1.40 | 740 | 590 | RTCD2892W271KR045M |
|  |  | 35*35 | 0.15 | 1.50 | 740 | 590 | RTCD2892W271KS035M |
|  | 330 | 30*50 | 0.15 | 1.71 | 610 | 490 | RTCD2892W331KR050M |
|  | 390 | 35*45 | 0.15 | 1.90 | 520 | 415 | RTCD2892W391KS045M |
|  | 470 | 35*50 | 0.15 | 2.21 | 430 | 342 | RTCD2892W471KS050M |
|  | 560 | 35*60 | 0.15 | 2.25 | 360 | 320 | RTCD2892W561KS060M |
|  | 680 | 35*65 | 0.15 | 2.90 | 320 | 260 | RTCD2892W681KS065M |
| 500 2H (550) | 100 | 30*25 | 0.15 | 0.92 | 1995 | 1600 | RTCD2892H101KR025M |
|  | 120 | 30*30 | 0.15 | 1.00 | 1665 | 1330 | RTCD2892H121KR030M |
|  |  | 35*25 | 0.15 | 1.00 | 1665 | 1330 | RTCD2892H121KS025M |
|  | 150 | 30*35 | 0.15 | 1.21 | 1330 | 1065 | RTCD2892H151KR035M |
|  | 180 | 30*40 | 0.15 | 1.42 | 1110 | 890 | RTCD2892H181KR040M |
|  |  | 35*30 | 0.15 | 1.31 | 1110 | 890 | RTCD2892H181KS030M |
|  | 220 | 30*45 | 0.15 | 1.62 | 910 | 730 | RTCD2892H221KR045M |
|  |  | 35*35 | 0.15 | 1.53 | 910 | 730 | RTCD2892H221KS035M |
|  | 270 | 30*50 | 0.15 | 1.80 | 740 | 595 | RTCD2892H271KR050M |
|  |  | 35*40 | 0.15 | 1.71 | 740 | 595 | RTCD2892H271KS040M |
|  | 330 | 35*45 | 0.15 | 2.00 | 610 | 485 | RTCD2892H331KS045M |
|  | 390 | 35*50 | 0.15 | 2.30 | 520 | 415 | RTCD2892H391KS050M |